## Slide 1: Unconventional ferroelectricity and its polarization switching dynamics in moiré system
Presenter: Kyoungpyo (KP) Lee
Physics Concerto, March 5th, 2025

## Slide 2: Outline
What is Ferroelectricity?
  Ferroelectricity: introduction
  Ferroelectric domains and domain wall
  Polarization switching dynamics
Moiré ferroelectricity: a new type of ferroelectricity
  Origin of Moiré ferroelectricity
  Novel polarization switching: domain wall sliding
Moiré ferroelectrics as functional platform
  Functional platform for physics
  Engineering application

## Slide 3: Outline
What is Ferroelectricity?
Moiré ferroelectricity: a new type of ferroelectricity
Moiré ferroelectrics as functional platform

## Slide 4: Outline
What is Ferroelectricity?
  Ferroelectricity: introduction
  Ferroelectric domains and domain wall
  Polarization switching dynamics
Moiré ferroelectricity: a new type of ferroelectricity
Moiré ferroelectrics as functional platform

## Slide 5: Ferroelectricity (FE): Introduction
Dielectric susceptibility of material
Highly nonlinear susceptibility leads to a remnant electrical polarization in the zero-field limit.
W. Lee et al. APL Materials 9.12 (2021).
Toprasertpong, Takenaka, & Shinichi Takagi. Applied Physics A 128.12 (2022): 1114.

## Slide 6: Ferroelectricity (FE): Introduction
Energetic perspectives on FE: Polarization order driven by spontaneous inversion symmetry breaking
Linear
dielectric
Paraelectric
Ferroelectric
LDE or PE
FE
W. Lee et al. APL Materials 9.12 (2021)

## Slide 7: Ferroelectric domains
Domain: A large cell in which every polarization aligns along a certain direction.
Alikin et al. Materials 10.1 (2017): 47.
W. Lee et al. APL Materials 9.12 (2021).

## Slide 8: Ferroelectricity-driven fields
Depolarization field (): a built-in field generated by bound charge
Stray field (): a surrounding field generated by ferroelectric potential
Two ways to minimize
D. M. Evans et al. Physical Sciences Reviews 5.9 (2020).

## Slide 9: Ferroelectric domain wall
Domain wall: Line (1D) or surface (2D) boundary between one domain and the other.
Scott et al. Applied Physics Reviews 4.4 (2017).
W. Lee et al. APL Materials 9.12 (2021).

## Slide 10: Domain wall characteristics
Types of domain wall: Ising, Bloch, Néel
Charge trap in the domain wall affects FE characteristics.
D. M. Evans et al. Physical Sciences Reviews 5.9 (2020).

## Slide 11: Polarization switching
, da Silva et.al, Tech. App. Nano. (2022)
W. Lee et al. APL Materials 9.12 (2021).
S. Kunda et al. Scientific reports 5.1 (2015): 12415.
Displacive Ferroelectrics

## Slide 12: Outline
What is Ferroelectricity?
Moiré ferroelectricity and domain network
  Towards a new type of ferroelectricity
  Origin of Moiré ferroelectricity
  Novel polarization switching dynamics
Moiré ferroelectrics as functional platform

## Slide 13: Towards a new type of ferroelectricity
C. N. Lau, K. F. M. W. Bockrath, K. F. Mak*, F. Zhang*, Nature 602, 41–50 (2022)
Dry transfer / tear-and-stack method
Can we artificially generate ferroelectricity?
Moiré lattice
Local inversion symmetry breaking
D. Huang, J. Choi, C. K. Shih*, X. Li*, Nat. Nanotech. 17, 227–238 (2022).

## Slide 14: Towards a new type of ferroelectricity
Moiré potential as a hint
  observed in MoS2/WSe2 heterobilayer
Scanning Tunneling Microscopy (STM)
C. Zhang, C.K. Shih* et al. Sci. Adv. 3, e1601459 (2017)
X. Liu, A. Yazdani* et al. Nat Comm. 12, 2732 (2021)

## Slide 15: Origin of Moiré ferroelectricity
Boron
Nitrogen
D.S. Kim, X. Li* et al. Nat. Mater. 23, 65–70 (2024).

## Slide 16: Origin of Moiré ferroelectricity
Predicted potential profile based on electronic charge redistribution.
D.S. Kim, X. Li* et al. Nat. Mater. 23, 65–70 (2024).

## Slide 17: Polarization switching in moiré system
How to switch moiré FE domains using electrical field?
Possible mechanism of polarization switching
  Charge “re-redistribution” under the applied field
  Domain wall sliding due to the mechanical shift in stacking geometry
  Well…?
Still ongoing investigation!

## Slide 18: Polarization switching in moiré system
Domain wall sliding in an isolated (or wall-pinned) domain
V. Stern, M. Ben Shalom* et al. Science 372, 1462–1466 (2021)

## Slide 19: Polarization switching in moiré system
Domain expansion/shrinkage in the domain network
  Almost no hysteresis observed in a pure moiré domain network.
K. Ko, P. Kim*, H. Yoo* et al. Nat. Mater. 22, 992–998 (2023).
Operando Trasmission Electron Microscopy (TEM)

## Slide 20: Polarization switching in moiré system
Network-based global switching
KP Lee, X. Li*, in progress

## Slide 21: Outline
What is Ferroelectricity?
Moiré ferroelectricity: a new type of ferroelectricity
Moiré ferroelectrics for applications
  Functional platform for physics
  Engineering application

## Slide 22: Moiré ferroelectrics as functional platform
D.S. Kim, X. Li* et al. Nat. Mater. 23, 65–70 (2024).

## Slide 23: Remote engineering of electronic states
D.S. Kim, X. Li* et al. Nat. Mater. 23, 65–70 (2024).
Device structure
Optical sensing of new stark-shifted exciton in Moiré FE domain wall.

## Slide 24: Remote engineering of electronic states
Zhang et al. arXiv preprint arXiv:2406.18028 (2024).
Moiré FE domain-assisted plasmonic excitation in graphene/t-hBN
Scanning near-field
Optical microscopy

## Slide 25: Devices for engineering application
A new stark-shifted exciton in Moiré FE domain wall.
K. Yasuda, P. Kim*, R. Ashoori* et al. Science (2024): eadp3575.

## Slide 26: Thank you!